## Slide 1: X-ray Image Analysis Approach for Lithium-ion Battery Cells
Wenhao, Xu, 31/01/18
Master Thesis

## Slide 2: Agenda
  Image processing workflow
  Image selection
  Edge extraction workflow(X-direction)
  Region of interest extraction
  Fake edge removal
  Electrode edge positioning through interpolation
  Edge extraction workflow(Y-direction)
  Problems and suggestions

## Slide 3: Image processing workflow

## Slide 4: Image selection: X-direction images
Function: images_to_process
Input: main path of images
Output: path of X-, Y-, and Z-direction images
The images in main path should be firstly classified into X, Y, and Z folders, otherwise this script doesn’t work

## Slide 5: Image selection: X-direction images
The X-images on both narrow and broad side are with electrode length more than 680 pixel
electrode length>680
X-ray

## Slide 6: Image selection: Y-direction images
Images with minimal 50 pixels of distance to the image boundary are selected

## Slide 7: Image selection: Z-direction images
10 images according to a constant interval from the Z-image sequence are selected

## Slide 8: Edge extraction workflow

## Slide 9: Region of interest extraction
Input: battery cell images, grayscale threshold, anode length
Output: anode and cathode regions, start column of the anode
Result of setting threshold = 10; anode_length = 70;
threshold = 10
anode_length
start_column_of_anode
Cathode
Anode

## Slide 10: Fake edge removal
True edges:
The brightness in the left part should be larger than the right part
Set rules to remove fake edges:
mean brightness on the left - mean brightness on the right >30
Extract the local region of electrode edge and examine if the region has the edge features
the local region of electrode edge

## Slide 11: Electrode edge positioning through interpolation
Curve fitting through Harris points
Extract 15 points equidistantly from the curve
Not all the electrode edges can be correctly extracted, thus we create a curve based on the already extracted edge points, and then extract the rest edge points from the curve.

## Slide 12: Edge extraction workflow(Y-direction)
Similar to the workflow for X-direction images

## Slide 13: Problems and suggestions
Image selection (lack of standardization in image acquisition)
ROI extraction(hard to divide anodes from cathodes when analyzing abnormal images)
Edge extraction through interpolation

## Slide 14: Problems: image selection
Image acquisition lack of standardization causes trouble for image selection
Missing anodes on the top
Missing anodes on the bottom

## Slide 15: Problem: image selection
Suggestions:
Manual image selection.
Develop a GUI to select the images and verify if the images are properly selected.
When all the images are acquired in a same manner, it is possible to select images automatically using the method I used in the scripts, only thing to do is to adjust some parameters in the script.

## Slide 16: Problem: ROI extraction
Abnormal cathodes make it very hard to divide anodes from cathodes
Suggestions:
  GUI based ROI extraction
  Select a proper anode length respectively when analyzing images from different battery cell
anode_length

## Slide 17: Problem: Edge extraction through interpolation
Image: zelle5_slices_X_1011
In the scripts the cathode on the top will be judged as the first cathode
However, in this case, the vertical position of the first cathode is lower than the second cathode, this cause problems in sorting the cathodes and the script judged the actual first cathode as the second cathode.
This causes problems in interpolation
Second cathode
First cathode

## Slide 18: Problem: Edge extraction through interpolation
wrong
right
What I have done is to manually adjust the vertical position of the first cathode and make sure the first cathode being correctly recognized, and it is accomplished in interpol_fix script.
It is suggested to develop a method that can recognize the electrode edge correctly.
Wrong cathode recognition result in inaccurate electrode edge position